New approach for consideration of adsorption/desorption data

Mihaela-Cristina Băleanu*,   Raoul R.Nigmatullin**, Salih Okur***, Kasim Ocakoglu

* Faculty of Physics, University of Bucharest , P.O. Box MG-7, Măgurele 077125, Romania

Mihail Sadoveanu Theoretical High School, District 2, Bucharest 021586, Romania

( e-mail: cris_balance@ yahoo.com)

** Kazan (Volga Region) Federal University, Kazan 420008, Tatarstan, Russia

(e-mail:nigmat@knet. ru)

***Izmir Institute of Tehnology, Faculty of Science,Izmir, TR-35430,Turkey

(e-mail:salihokuru@iyte.edu.tr

Tarsus Technical Education Faculty, Mersin University, 33480

Tarsus, Mersin Turkey (e-mail: kasim.ocakoglu@mersin.edu.tr)

Abstract: In this paper we proposed a new Langmuir model and we have tested it on the humidity adsorption and desorption kinetic data of spin coated 50 nm Ruthenium polypridyl complex (Ru- PC K314) film has been measured under relative humidity between 11 % and 97 % using by Quartz Crystal Microbalance (QCM) procedure.

Keywords: QCM, Langmuir model, Eigen-Coordinates,adsopriton, desorption, Ruthenium polypridyl complex.

- INTRODUCTION

The humidity adsorption and desorption kinetic data of spin coated 50 nm Ruthenium polypridyl complex (Ru- PC K314) film has been measured under relative humidity between 11 % and 97 % using by QCM technique. QCM have been extensively used for the determination and investigation of the kinetics of adsorption/desorption of adsorbate molecules Hartmann et al. (1996); Kalchenko et al. (2002) for monolayer films. QCM technique denotes a powerful approach for determining the sensing properties of materials before a sensor device design during development stages.

Langmuir model has been used successfully for monolayer

films to analyze adsorption kinetics. In (Su et all.(2006)) a novel ceramic nanowires of TiO2 and poly(2-acrylamido-2-methylpropane sulfonate) composite material films coated QCM was prepared as a low humidity sensor.

The swelling behaviour of a series of hydrophilic random copolymer coatings in controlled humidity environments and in water were investigated. Swelling data were obtained from a QCM and from spectroscopic ellipsometry was investigated by Chen et al.(1999). In (Ayad et al.(2009)) thin films of polyaniline base, emeraldine base (EB),coating on the quartz crystal microbalance (QCM) electrode have been used as a sensitive layer for the detection of a number of primary aliphatic alcohols such as ethanol, methanol, 2-propanol and 1-propanol vapours.

A QCM coated with Nafion® film recast from Nafion®(Ag) complex solution has been used to investigate the interaction between methanol, water and Nafion®(Ag) and to determine simultaneously the concentration of methanol and water (relative humidity) was reported in Sun and Okada (2000).

The manuscript is organized as follows.

In section 1, we will give more information about the experiment. In section 2, we briefly discuss about the Langmuir model which was first introduced in 1916. In section 3, the experimental details are described for the humidity adsorption and desorption kinetic data of spin coated 50 nm Ruthenium polypridyl complex (Ru-PC K314) film. In section 4 we suggest the generalized Langmuir model which received the experimental confirmation.  Section 5 constitutes a brief conclusion of the paper.

2. QCM ADSORPTION AND DESORPTION KINETICS

QCM has been used frequently to measure the fractional coverage θ as a function of time during the adsorption and desorption of water vapor molecules by Calix[4]arene film, while the increase in the frequency shift reflects the molecular mass uptake or loss. Hence the difference between the oscillation frequency shift (Δ) of coated and uncoated QCM is directly proportional to the adsorbed mass of moisture molecules. The simplest relationship between the surface adsorption kinetics and frequency shift (Δ) of QCM can be expressed as following:

(1)

where Δf  is the QCM  resonance frequency , t is time ,  and are the adsorbtion and desorbtion rate constants and C is the water vapor concentration in the air. During the adsorption process, Δf  is equal to Δfmax  for very long time.

3. EXPERIMENTAL

For the preparation of QCM electrodes, gold coated quartz crystal electrodes were placed into ethanol and ultrasonically cleaned, then rinsed by de-ionized water. 1 mg/ml Ru-PC was dissolved in deionized water. 5μl of solution was spin-coated on to quartz crystal with 2000 rpm. After drying at room conditions, it was kept in dessicator at room temperature for 3 hours. Then the quartz crystal coated with Ru-PC film was used to record both the reference frequency at 11 % and the frequency changes up to 97 % relative humidity. The thicknesses of films were measured using a Dektak profilometer from Veeco and found to be 50 nm. A Time-Resolved Electrochemical Quartz Crystal Microbalance (EQCM) with the model of CHI400A Series from CH Instruments (Austin, USA) has been used to measure the change in the resonance frequency of quartz crystals between gold electrodes via both serial and usb interface connected to a computer. The QCM works with oscillation frequencies between 7:995 MHz - 7:950MHz. The density (ρ) of the crystal is 2:684 g=cm3, and the shear modulus (μ) of quartz is 2:947 × 1011 g=cm:s2. Around oscillation frequency of 7:995-MHz, a net change of 1 Hz corresponds to 1:34 ng of materials adsorbed or desorbed onto the crystal surface of an area of 0:196 cm2.

The signals coming from a QCM electrode and a commercial RH humidity sensor were simultaneously measured during the adsorption and desorption process. Both the relative humidity and temperature were also recorded during measurements while maintaining the temperature around 23◦C. For this purpose, a EI-1050 selectable digital relative humidity and temperature probe with a response time of 4 s and a resolution of 0:03 % RH was used with a USB controlled LabJack U12 ADC system combined with a single chip sensor module (SHT11) manufactured by Sensirion (Staefa, Switzerland).

The detailed information about the synthesis of [RuII ( bis(4; 7-diphenyl-1; 10−phenanthroline-disulfonic acid disodium salt) (4; 4′-dicarboxy-2; 2′-bipyridine)], (Ru-PC K314) can be found in Ocakoglu and Okur (2010). For further information, see this reference.

Fig. 1. Chemical structure of ruthenium polypridyl complex

4. LANGMUIR MODEL AND ITS MODIFICATION

In this paper, we deal with Langmuir model which was first

developed in 1916  by Irving Langmuir , Langmuir (1916);

Kankare and Vinokurov (1999); Kapoor et al. (1990). In order to analyze the adsorption and desorption kinetics of gas vapor molecules onto organic or inorganic films, Langmuir adsorption isotherm model is applied Sauerbrey (1959); Karpovich et al. (1994); Gregg and Sing (1967); Sun et al. (2007); Su and Chang (2008). As a result the model describes the rate of surface reaction for forming a monolayer on the surface by using the below equation,

.				      (2)

Here θ is a unitless quantity, which means the fraction of surface coverage, Ka and Kd denote the rate constants for the adsorption and desorption processes.

In this study QCM has been used to measure the fractional coverage θ a function of time during the adsorption and desorption of water vapor molecules.

Hence the difference between the oscillation frequency shift Δf of coated and uncoated QCM is directly proportional to the adsorbed mass of moisture molecules. The relationship between the surface adsorption kinetics and frequency shift (Δf) of QCM can be expressed by expression (1)

As one can notice from comparison of expressions (1) and (2) they are similar to each other and so the frequency shift (f

is directly proportional to (. The fitting of experimental data realized with accordance of expression (2) by the Eigen-Coordinates (ECs) method gives unsatisfactory results. We see at least two possible reasons (a) experimental data are not so clean and always contains some uncontrollable factors; (b) the experimental data contains more than one exponential function and so the simplest model (2) should be modified and generalized. In order to see possible modifications let as present Eqn.(2) in the form of the finite difference equation

(3)

Equation (1) can be rewritten in complete analogy with Eqn.(3). Equation (3) expresses in the simplest form the linear principle of the strongly-correlated variables. Equation (3) can be easily generalized if we present this equation in the form

(4

This equation has a simple physical meaning. It signifies that the adsorption/desorption phenomenon can be divided on some stages related on a structure of a surface (which in the most cases represents a random fractal surface) and the geometrical configuration of the adsorbed/desorbed molecules. The physical meaning of the constants an should be related with relative concentrations of the molecules and character of the surface that participate in this phenomenon. Their exact dependence on concentration and fractal dimension of the surface considered will be a subject of the further research. In this paper we only verify this general relationship on available data. The solution of the functional equation was considered in paper (Nigmatullin (2008). It is expressed in the form of linear combination of exponential functions

(5)

Here the constant b is expressed in the form

(6)

The unknown exponential constants (n are found as roots of the characteristic polynomial

(7)

En(t) in (5) can be expressed approximately in the form of periodical functions with period T.

(8)

Here an, bn and (n are some fitting constants. The value <m> defines the leading mode. The fitting to function (5) can be realized with the help of the ECs method (Nigmatullin  (1998)) that helps to reduce the non-linear fitting procedure to the conventional linear least square method (LLSM). For verification of the hypothesis (4) we chose the minimal number of components (items) k=3. The fitting function identified by the ECs method is written as

(9)

This fitting function (9) contains 6 fitting parameters and describes all available data with acceptable accuracy. The accuracy of adsorption data is located in the interval: [0.04 % < RelErr(%) < 0.07%] as for the desorption data the accuracy is in the interval. [0.15% < RelErr(%) < 0.34%].

Fig.2. The fit of the adsorption curves realized for two cycles.

Fig.3. The fit of desorption curves realized for two cycles with function (9).

The set of the fitting parameters are given in Table 1. Notations are taken from expression (9)

Table 1.

| Cycle | A0,A1 | A2,A3 | (1,(2 | ( |
| --- | --- | --- | --- | --- |
| Ad1 | 96.971 -0.9397 | -13.247 -59.227 | -6.8904 -2.2149 | 10.709 |
| Ad2 | 98.647 0.2634 | 0.69817 -71.822 | -0.54768 -2.1982 | 10.206 |
| Ad3 | 97.677 3.1639 | 8.325 -93.886 | -5.5395 -2.6999 | 12.668 |
| Des1 | 3.4147 0.86231 | -0.33054 50.218 | -0.41477 -6.7359 | 8.8866 |
| Des2 | 1.664 0.05576 | -0.12518 34.386 | 2.6103 -5.2821 | 12.703 |
| Des3 | 2.0239 3.2448 | 2.3631 58.115 | -0.09221 -11.461 | 2.3575 |

Ad=Adsorption,Des=Desorption

5. CONCLUSIONS

Finding new generalization of the Langmuir model is an interesting problem. In this paper we investigated the humidity adsorption and desorption kinetic data of spin coated 50 nm Ruthenium polypridyl complex (Ru-PC K314) film within a new method.

The obtained results definitely show that the Langmuir equations can be generalized by making use of the ECs method. The experimental confirmation of the hypothesis (9) that follows from solution of the functional equation (4) implies that some important factors participating in adsorption/desorption phenomena can be taken into account.

REFERENCES

Ayad, M.M., El-Hefnawey, G. and  Torad, N. L.(2009).

A sensor of  alcohol vapours based on thin polyaniline base film and quartz crystal microbalance. J. Hazard. Mat. 168 , 8588-	8597.

Chen,W-L, Shull, K.R., Papatheodorou,T., Styrkas,D.A. and Keddie,J.L.(1999). Equilibrium Swelling of Hydrophilic Polyacrylates in Humid Environments. Macromolecules 32, 136-144.

Gregg, S. J., and  Sing,K.S.W.(1967) Adsorption, Surface Area and Porosity. Academic Press.

Hartmann, J., Auge, J., Lucklum, R., Rosler, S., Hauptmann, P., and Adler, B.(1996). Supramolecular interactions on mass sensitive sensors in 261 gas phases and liquids. Sens. Actuat. B: Chem. 34, 305–311.

Kalchenko, V. I., Koshets,I.A., Matsas,E. P., Kopylov, O. N., Solovyov, A.,  Kazant, Z. I., Seva,O., and Yu.M. Shirshov, Yu. M.(2002). Calixarene-based qcm sensors array and its response to 265 volatile organic vapours. Mater. Sci., 20(3),73–88.

Kankare, J., and  Vinokurov.I.A. (1999). Kinetics of langmuirian adsorption onto planar, spherical, and cylindrical

surfaces. Langmuir  15, 5591–5599.

Kapoor, A., Ritter,J.A., and Yang, R. T.(1990). An extended Langmuir model for adsorption of gas mixtures on

heterogeneous surfaces. Langmuir  6(3), 660–664.

Karpovich, D.S.,Blanchard,G.J. (1994). Direct

measurement of the adsorption kinetics of alkanethiolate

self-assembled monolayers on a microcrystalline gold

surface. Langmuir 10, 3315–3322.

Langmuir, I. (1916). The constitution and fundamental properties of solids and liquids. J. Am. Chem. Soc.  38:2221–2295.

Nigmatullin, R.R. (2008). Strongly Correlated Variables and Existence of the Universal Distribution Function for Relative Fluctuations. Phys.  Wave Phen.16. 119-145.

Nigmatullin, R.R. (1998). Eigen-Coordinates: New method of identification of analytical functions in experimental measurements. Appl. Magn. Reson., 14, 601-633.

Ocakoglu, K. and  Okur, S. (2010). Humidity sensing properties of novel ruthenium polypridyl complex. Submitted to Sens. Actuat. B.: Chem.

Sauerbrey, G. (1959).Verwendung von schwingquarzen zur wagung dunner schichten und zur mikrowagung. Z. Phys 155, 206–222.

Su,P-G, Sun, Y-L, and Lin,C-C. (2006). Novel low humidity sensor made of TiO2 nanowires/poly(2-acrylamido-2-methylpropane sulfonate) composite material film combined with quartz crystal microbalance. Talanta 69, 946951.

Sun,L-X., and  Okada,T. (2000). Simultaneous determination of the concentration of methanol and relative humidity based on a single Nafion (Ag)-coated quartz crystal microbalance. Anal. Chim. Acta  421, 8392-8399.

Sun,Y. L., Wu,R. J., Huang,Y. C., Su,P.G., Chavali,M., Chen, Y.Z. and Lin. C. C. (2007).  In situ prepared polypyrrole for low humidity qcm sensor and related theoretical calculation. Talanta 73151,  857–861.

Su, P. G., and Chang, Y. P. (2008). Low humidity sensor based on a quartz-crystal microbalance coated with polyprrole/ag/tio2 nanoparticles composite thin films. Sens. Actuat. B: Chem. 125, 915-920.